# Text boxes

##### Ledger Panel: Colorado Canyon

M S International, Inc.

Premium Surfaces Since 1975

#### Packaging

- Panels:   8 pcs/box; 240 pcs/crate

- Corners: 4 pcs/box;   80 pcs/crate

Color: 		Beige, Brown

Application: 	Walls, barbeque areas, etc.

###### Technical Information

- Flat panel:  6 x 24”

- Corner:       6 x 18 x 6”

- Thickness:  0.75-1”

- Appox. Weight:  8.5 lbs.

- Type: 	Marble

- Finish:  Splitface

- Average Compressive Strength:

Dry/5200 Psi

#### Adhesive

- Exterior application: a flexible latex based mortar system suitable for the stone is recommended.

- Interior application: a thin set mortar suitable for the stone is recommended.

- For light colored stones, a white mortar is recommended.

## Substrates

## Exterior/Interior

- Fully cured concrete (at least 28 days cured)

- Masonry brick

- Regular brick

- Cement mortars

- Cementitious backer units

## Interior only

- Gypsum plaster (max 10’ high)

- Gypsum wallboard (max 10’ high)

- Exterior grade plywood (max 10’ high)

- Cementitious backer units